Template for Submission of Manuscripts to American Chemical Society Journals

Word 2010, single-column, double-spaced (2013)

This template is a guide to be used to prepare manuscripts for submission. Please consult the Instructions to Authors or a recent issue of the journal for detailed guidelines and procedures for submission. This template is intended to benefit to the author in that the entire manuscript (text, tables, and graphics) may be submitted in one file. Inserting graphics and tables close to the point at which they are discussed in the text of the manuscript can also be a benefit for the reviewer.

When you submit a manuscript using this template, you will not actually see the page formatting that appears in the printed journal. This will occur as part of the editorial production process. Abbreviated instructions for using the template follow. Consult the documentation for your specific application and version for more information. Additional instructions can be found in the readme file at the web page where you downloaded this template.

Using the template

In ACS publications there are many different components of a manuscript (i.e., title, abstract, main text, figure captions, etc.) that are represented in the template.  See the Guide, Notes, Notice, or Instructions for Authors on the journal’s homepage to determine which parts should be included for the manuscript that you are preparing

- If typing your manuscript directly into the template, select (highlight) the text of the template that you want to replace and begin typing your manuscript (i.e., select the Title section for typing in your title).

- If you have already prepared your document in a Word file, you will need to attach the template to your working document in order to apply the Word Style tags. Further instructions can be found in the readme file at the web page where you downloaded this template.

- Go to the Add-Ins tab and you will see all the Word Styles from the template that has now been imported into the current document. A Styles toolbar has been generated that will display the different Styles for you to choose from. If this is not present, type in the following command (Alt+Ctrl+Shift+S) and it should appear. You can close this at any time and then reopen it when needed.

- Click in the sentence or paragraph and then go to the Add-Ins tab and select the relevant Word Style.  This will apply the Word Style to the entire text (sentence or paragraph). Do this for all sections of the manuscript.

- To insert graphics within the text or as a figure, chart, scheme, or table, create a new line and insert the graphic where desired. If your graphic is not visible, ensure that the Word Style is “Normal” with an automatic height adjustment. If the size of the artwork needs to be adjusted, re-size the artwork in your graphics program and re-paste the artwork into the template (maximum width for single-column artwork, 3.3 in. (8.5 cm); maximum width for double-column artwork, 7 in. (17.8 cm)). NOTE: If you are submitting a Table of Contents graphic, please insert the graphic at the end of the file.

- Ensure that page numbers are present on all pages before submitting your manuscript.

- Delete these instructions and any sections that are not needed.

- Save the file with the graphics in place: select Save As (File menu) and save it as a document file (not a .dot template file).

- Proof the manuscript to ensure that all parts of the manuscript are present and clearly legible.

Enhancing Confidence in Microplastic Spectral Identification via Conformal Prediction

Madeline E. Clough,a‡ Eduardo Ochoa Rivera,b‡ Andrew P. Ault,a Paul M. Zimmerman,a Anne J. McNeil*,a,c and Ambuj Tewari*b,d

a Department of Chemistry, University of Michigan, 930 North University Avenue, Ann Arbor, MI 48109-1055, USA

b Department of Statistics, University of Michigan, 1085 South University Avenue, Ann Arbor, MI 48109-1055, USA

c Macromolecular Science and Engineering Program, University of Michigan, 2300 Hayward Street, Ann Arbor, MI 48109-1055, USA

d Department of Electrical Engineering and Computer Science, 1301 Beal Avenue, University of Michigan, Ann Arbor, MI 48109-1055, USA

KEYWORDS microplastics, conformal prediction, spectral matching, hit quality index, spectral libraries

ABSTRACT Environmental microplastic identification is dominated by matching unknown spectra to libraries of standard spectra via database searching. In practice, a researcher chooses the library spectrum that is most similar to the unknown spectrum, where the likeness between the two spectra is expressed numerically as a hit quality index (HQI). Despite widespread use of HQI thresholds in the microplastic literature, in most instances, the acceptance of a spectral label lacks any associated statistical certainty. To address this gap, we report herein a statistical framework called conformal prediction that outputs a set of possible labels that contains the true identity of the unknown spectrum with a user-defined probability. Common microplastic reference libraries of environmentally aged and pristine natural and polymeric materials were used to illustrate the benefits of this approach when used with two similarity metrics to compute HQI. We present an adaptable workflow using our open-access code to ensure spectral matching confidence for the microplastic community, which should reduce manual inspection of spectral matches and enhance the robustness of quantification in the microplastic field.

SYNOPSIS Researchers rely on spectral similarity metrics to assign the polymer identity to unknown microplastic spectra. We present a statistical framework for enhanced spectral confidence and reduced manual evaluation in environmental microplastic quantification and identification.

GLOSSARY

Confidence – probability that the prediction set contains the correct identity of the unknown spectrum

Conformal prediction – machine-learning framework for uncertainty quantification

Efficiency – measure of average prediction set size, where a smaller prediction set is more efficient

Hit quality index – normalized score of spectral similarity returned by the similarity metric

Label – specific chemical identity in a reference library

Marginal – average confidence across all spectra, regardless of chemical classification

Prediction set – group of labels returned by the conformal prediction method

Prediction set size –number of labels returned by the conformal prediction method

Similarity metric – algorithm to compute spectral likeness

Introduction

Identifying microplastics (MPs) is essential to address health and environmental concerns caused by plastic production and pollution. Microplastics, defined as small pieces of plastic between one and 5000 micrometers, have been found in environmental matrices such as seawater, freshwater, soil, and air. The extent of microplastic pollution and their major sources need to be identified to develop remediation solutions and institute future regulations. Many researchers have employed techniques such as Fourier transform-infrared (FT-IR) or Raman spectroscopy to determine a microplastic’s identity and origin.

In this context, automated spectral matching has prevailed as a solution to time-intensive manual spectral matching of unknown environmental species to standard reference polymers. Commercial software equipped with spectral library-searching modules, such as Bruker’s OPUS, Thermo Fisher’s OMNIC, and Wiley’s KnowItAll (KIA), have been employed to produce a similarity score between an unknown spectrum and a reference spectrum.,, Oftentimes, this score of spectral likeness, which can be computed via similarity metrics, is referred to as hit quality index (HQI).7 Researchers commonly use a threshold value of HQI that must be met or exceeded to label unknown spectra with a polymer classification. However, there is disagreement in the literature regarding the meaning expressed by a HQI value, occasionally being referenced as a measure of confidence in a polymer label.,, This assertion of confidence is misleading, as the HQI does not provide any measure of statistical certainty. Rather, the score simply reflects a measurement of similarity between two spectra using metrics such as Pearson correlation coefficient (PCC) and Euclidean distance.

Because many polymers exhibit similar structures (and therefore spectra), and vibrational spectra can change due to environmental aging, labeling unknown spectra using similarity metrics alone is problematic. A better approach for robust MP quantification and sourcing would include an indication of statistical certainty in spectral matching. Acceptance of an identity with an HQI score above an arbitrary threshold may lead to misidentification, as indicated by the findings of Lopez-Rosales et al., wherein a threshold of 0.85 led to an overestimation of MP counts. Indeed, voices in the MP community have called for stricter assurances of correctly labeling polymer identity through manual assessment of likeness between unknown spectra and standard references.16,

To answer this call for increased confidence, some researchers have framed uncertainty in spectral labeling via distributions of errors between automated spectral match scores and expert manual assessments,, as well as automated correlation scores of samples with known composition., These approaches provide an uncertainty quantification for the whole sample (often expressed as a false negative rate when environmental plastic spectra are not matched to polymer references), but for individual spectra they are limited to the acceptance or rejection of a single classification. Moreover, these methods are asymptotically valid, meaning the guarantees are only valid when the number of observations nears infinity. In contrast, methods such as conformal prediction quantify the uncertainty of individual matches and output a set of labels with a guaranteed confidence (or probability) that this set contains the true identity of the query spectrum.

Conformal prediction (CP) ,  is a framework that provides a systematic and principled approach to quantifying prediction uncertainty. Practically, this method generates a prediction set of labels that guarantees a specified level of finite sample confidence, meaning the probability that the correct label is included in the prediction set is equivalent to the user-defined confidence. CP has been increasingly popular in machine learning, where it is able to provide uncertainty quantification for a model without the need for retraining, which can be a computationally intensive procedure.  Our introduction of CP to the MP community herein provides uncertainty quantification by setting a spectral matching threshold with a statistical guarantee.

In CP, the choice of the similarity metric (e.g., PCC) is crucial because, while the confidence guarantee holds for any similarity metric, different similarity metrics may lead to more or less informative, or efficient, predictions. The efficiency of the prediction set relates to the number of labels returned, where a more efficient metric would return fewer labels. Thus, exploring different similarity metrics is necessary to compare the efficiency of resultant prediction sets. This aspect of CP led us to investigate the nearest neighbor (NN) similarity metric  in addition to the usual correlation-based HQI, improving size of the prediction sets without changing the confidence level.

Herein, we first evaluate the spectral correlation software, methods, and thresholds reported in the recent microplastic literature to establish a baseline of automated matching practices in the MP community. We then illustrate that the HQI scores generated by a commonly used commercial software lack the clarity needed to confidently label MPs. Lastly, we demonstrate the advantage of using CP in tandem with similarity metrics such as PCC and NN to provide a user-specified level of confidence associated with a label prediction set. Through this work, we aim to provide a workflow to incorporate confidence in microplastic spectral matching and establish guidance for HQI thresholding and label acceptance for more robust environmental MP identification.

Methods

Literature Review

To illustrate the microplastic community’s recent use of library searching software, metrics, and thresholds, we conducted a Web of Science search for articles published within the last eight months at the time of searching (May 2023 to January 2024). To limit entries, we specifically targeted papers involving MP identification in an oceanic matrix. As this matrix has received the greatest attention of all environmental sectors, we expect that the methods used in these articles will best reflect the current state of microplastic spectral matching. Parameters of our search included the topics of “microplastic*” and “spectroscopy” and “marine”. Ninety-six results were returned by the database. For each returned record, the data analysis routine was noted. When spectral database matching was used, the software, matching metric, and threshold were recorded. Publications were excluded from the tabulated results when neither FT-IR nor Raman techniques were employed and/or when no unknown MPs were evaluated (Scheme S1).

Commercial Software Library Searching

The open-access spectral databases “FT-IR library of plastic particles” (FLOPP) and “FT-IR library of plastic particles sourced from the environment” (FLOPP-e) were chosen for commercial software matching due to their availability and widespread use in the microplastic community. All individual spectra belonging to the polyethylene (PE) and polypropylene (PP) classes available in the FLOPP-e library were downloaded as .csv files and uploaded to Wiley’s KnowItAll SearchIt function. These polymers were chosen because they had the greatest number of example spectra in the environmentally aged library (49 and 66, respectively). For each spectrum, transmission mode was indicated, and a single component search was performed using the default settings of correlation method and optimized corrections. A spectral inclusion window was drawn from 4000 to 650 cm-1 to include only regions of the spectra where data had been collected.27 Each spectrum was searched for correlation with pristine polymers in the FLOPP library and the hit list was documented. The highest score and label as well as the number of matches and number of polymer classes yielding HQI ≥ 70 were recorded.

Similarity Metrics Used to Compute Hit Quality Index

In this work, two different metrics were employed for spectral matching. Both metrics treat the spectra as multi-dimensional vectors and compute the corresponding metric to library reference spectra. The similarity metric between the vectors is normalized to output a hit quality index between zero and one, where a value of zero represents complete dissimilarity and a value of one indicates an exact match.7 The first metric we employed is the widely known Pearson correlation coefficient, described by equation 1, which is less influenced by signal intensity differences and more heavily impacted by differences in spectral band patterns.7,

PCC= covxtest,xrefσtestσref #1

Where covxtest,xref,σtest,σref are the covariance between spectra xtest and xref, the standard deviations of xtest and xref, respectively.

We also explore a less common similarity metric in the microplastic literature, which is related to the nearest neighbor classification model. This metric, similar to the Euclidean distance metric, is not bounded between [0,1] and the match is determined by the lowest value. Hence, a transformation is needed to make it a proper similarity metric (see Supporting Information). The nearest neighbor similarity metric is defined as:

NN=xtest - xrefminy{xtest - x:y≠yref} #2

Where xtest - xref is the Euclidean distance between spectra xtest and xref and x is the closest spectra with respect to xtest corresponding to the label y. For both PCC and NN metrics, we used the standard normal variate (SNV) for all analyzed spectra (see Supporting Information section II). Use of SNV enables the predicted classification labels of NN and PCC to be the same, and thus the uncertainty about their predictions is comparable.

Conformal Prediction

Conformal prediction is used to generate prediction sets (here, polymer labels) for new observations given a trained prediction model (in our case, the spectral reference library) that provides both a label and a heuristic uncertainty score given by the chosen similarity metric. The prediction set is achieved using a calibration dataset that represents the variability of unknown spectra to be classified while guaranteeing a certain level of confidence. As CP only requires mild assumptions to achieve statistical guarantees, (see Supporting Information) the framework can easily be instituted for more robust spectral classification.

In brief, the true positive (FLOPP-e spectrum label matching to a FLOPP spectrum of the same label) similarity scores of a calibration set representing 90% of the environmentally aged FLOPP-e plastic spectra was compared to FLOPP reference spectra and the resultant HQI values were tabulated in two frequency distributions relating to PCC and NN.  Next, the remaining 10% of FLOPP-e spectra were used as a test set, in which the HQIs for each spectrum’s similarity to reference polymers in the FLOPP library were calculated.  The HQI values from the test spectra for each reference polymer label were compared to the threshold defined by the corresponding quantile of the calibration set distribution that resembles the user-defined theoretical confidence (here, 90%) for both PCC and NN. If the similarity score for a polymer label was above the threshold, meaning that only 10% of the calibration data’s true positive scores were calculated to be smaller than the similarity score, then the label was added to the prediction set with an associated 90% theoretical confidence (Scheme 1). In the instance where multiple labels are included in the prediction set, they are ordered from highest to lowest observed HQI.

Scheme 1. Conformal prediction methodology workflow.

We calculated the empirical confidence and set size (number of labels included in the prediction sets) for all test data. The CP methods were repeated 500 times with different random splits of the calibration and test data in a cross-validation (CV) fashion, and the mean quantities of empirical confidence and prediction set size were calculated.

Class-Conditional Conformal Prediction

One limitation of the traditional CP framework is that the theoretical confidence guarantee is marginal, meaning that some labels may be under or over-guaranteed, as only the average theoretical confidence across all classes is assured. To address this issue, we also employ the class-conditional conformal prediction (CC-CP) approach. The basis of the CP methodology framework (i.e., create calibration set, determine threshold, compare test set to calibration distribution and add labels with HQI represented within the confidence region to the prediction set) remains the same. The only difference is that instead of constructing one distribution from the calibration set, we created a separate distribution for each label to ensure class-balanced confidence and similarity scores per polymer type were compared to label-specific distributions (Scheme S2). For this methodology, the FLOPP and FLOPP-e classifications were restricted to those with greater than 10 spectra available in the FLOPP-e libraries, limiting classifications to PE, PP, cotton (C), polystyrene (PS), and polyethylene terephthalate (PET). In practice, this indicates a notable trade-off between traditional CP and CC-CP. While CC-CP provides more robust predictions, it requires more data per label because it is necessary to build an HQI distribution for each label. The use of each method might depend on data availability and similarity between label dependent HQI distributions.

Results and Discussion

Literature Review

Similarity metrics used to label unknown spectra are not reported in the literature. We reviewed 96 recently published articles using vibrational spectroscopy to identify environmental MPs. Of these articles, 72 were used to establish a baseline of data analysis routines in the literature (see Supplemental Information section I). Database matching was the major (64%) routine identified, followed by manual evaluation (8%), and machine-learning techniques (4%) (Figure S1). Alarmingly, approximately 24% of published articles did not indicate how a spectral match was determined. Of the articles that indicated spectral database searching as the identification method, 74% did not report the similarity metric used to compute the match, which is concerning given that the algorithm chosen to analyze spectral similarity has a significant impact on the polymer classification.7,18,31 Approximately a quarter of the articles did report a similarity metric, with 22% using PCC and 4% using other algorithms (Figure S1). These results closely mimic the findings of Weisser et al. in 2022, where the proportion of articles that failed to detail the data analysis routine and similarity metric used for database matching remained unchanged in our 2024 study.7 It is concerning that there has been no observed response to their call for transparent communication of spectral identification methodologies. The constant proportion of researchers who have omitted critical information between these two evaluations continues to jeopardize the robustness and validity of these published MP identification findings.

There is no literature consensus on software used for spectral matching nor threshold of HQI to distinguish a microplastic. Applications specific to the parent company of the instrument used for identification were reported to perform automated spectral matching in 51% of analyzed publications (Figure 1a). KnowItAll, a commercial software for spectral matching from Wiley BioRad, was used in 19% of publications and open access searching platforms such as OpenSpecy, siMPle, and PlaMAPP were used in 24% of publications.  The default similarity metrics and preprocessing pipeline differ between the reported software, which obscures a direct comparison between HQI scores generated from different applications.18,31, A universal HQI threshold was likewise not supported by the literature (Figure 1b). While a threshold of 0.7 was reported by 42% of considered publications, the explanation for this choice, when reported, was dictated by precedent, likely because the seminal microplastic paper published by Thompson et al. in 2004 used this value of correlation to accept plastic identification. Approximately 31% of articles reported a higher threshold than 0.7 and about 20% of authors chose thresholds below 0.7, with 8% of publications using different criteria for automated match acceptance. In light of the ambiguity and diversity of software and thresholds used to aid spectral matching, it is clear that the MP community would benefit from a method to directly compare the performance of similarity metrics and guidance to determine a HQI threshold value with associated confidence.

Figure 1. Summary of 76 published MP papers regarding a) software applications used for automated spectral matching  and b) thresholds of HQI used to accept a match.

Commercial Software Library Searching

Similarity metrics alone do not guarantee confidence associated with a spectral match. We first searched all polyethylene and polypropylene FLOPP-e spectra using the FLOPP reference library in KnowItAll with the default correlation method and optimized corrections. The identity of the reference spectrum with the greatest HQI was recorded as the label for the unknown spectrum, as is typical for MP classification workflows. Overall, the FLOPP-e PE and PP spectra were matched to four unique polymer identities with the topmost HQI (Figure 2a). Thus, if the traditional approach of accepting the label of the reference spectra with the greatest HQI was followed, numerous spectra would be mislabeled. When expanding the criteria of a spectral match to include any label returned with a hit quality index ≥ 0.70, the cumulation of matches to individual PE and PP spectra returned seven and eleven unique labels, respectively (Figure 2a). It should be noted here that, as the FLOPP reference database contained 14 possible labels, 50% of available labels were assigned to PE spectra and 79% to PP spectra. It is clear that an HQI threshold is not accompanied by any measure of certainty, as reference spectra from multiple classes were matched to a single query spectrum with similar values of likeness. If we were to theoretically treat an HQI threshold as a level of confidence in a match, then that confidence would not be exclusive to the single classification with the greatest HQI; rather, it would include all labels above the chosen threshold. Therefore, the results of this experiment, which replicated libraries and software correlation methods used in the current MP literature, illustrate that the identifications output by these methods lack any associated certainty. In fact, a top match will always be generated for a query spectrum, regardless of whether a spectrum with the same classification is in the reference database.

Figure 2. Results from KnowItAll searches of PE and PP FLOPP-e spectra in terms of a) number of reference label classifications returned and b) proportion of misidentifications, where no ID is unidentified, C is cotton, PVC is polyvinyl choride, PEVA is polyethylene vinyl acetate, and R is rubber.

KnowItAll misidentifies ~20% of PE and PP spectra, largely due to chemical and spectral similarity between polymer classes. We recorded the proportion of misidentifications generated when the identity of reference spectrum with the greatest HQI is accepted as a label. The overall accuracy of KnowItAll’s assignments of FLOPP-e spectra to FLOPP references was ~80% for both PE and PP classes. However, we noted that there exists a risk of misidentification when following a standard protocol of accepting the spectrum label with the greatest HQI without further evaluation, as ~20% of spectra were misidentified within the FLOPP-e classes of PE and PP (Figure 2b). Individual spectra within the FLOPP-e or FLOPP library may suffer from a low signal to noise ratio or spectral artefacts known to influence the accuracy of a matching metric,36 which could account for instances of misidentification or when no labels were returned above the threshold (indicated as “no ID” in Figure 2b). However, we noticed that the greatest proportion of misidentifications seemed to have been caused by chemical, and thus spectral, likeness between the query and returned spectra. For instance, 70% of PE misidentifications were labeled as polyethylene vinyl acetate which features the same hydrocarbon repeat unit as PE (Figure 3a). The main spectral distinction between these two species is due to the copolymerized vinyl acetate unit in PEVA, which exhibits distinct peaks around 1725 cm-1 (C=O stretch) and 1228 cm-1 (C–O stretch). Similarly, 62% of PP misidentifications were classified as rubber. The chemical structures of PP and polyisoprene rubber likewise share chemical functionalities (Figure 3b). For instance, polyisoprene FT-IR spectra exhibit methyl and methylene bending and stretching vibrations which are spectrally similar to those observed in PP spectra.

Figure 3. Average min-max normalized overlayed spectra and chemical structures of a) PE (49 FLOPP-e spectra) and PEVA (10 FLOPP spectra) and b) PP (66 FLOPP-e spectra) and R (15 FLOPP spectra).

Current approaches to reducing misidentification of microplastics are tedious and lack any measure of associated confidence. Additional occasions of spectral likeness causing challenges in MP identification have been noted in the work of Schram and coworkers, where highly weathered PP was misidentified as chitin, and both PP and chitin were returned as labels with HQI greater than 0.7 for a less weathered PP sample.15 Further, the spectral differences of some polyamides and biological materials such as skin cells and proteins are so slight that these materials are likely to be misclassified when using traditional similarity metrics to output and accept a topmost HQI value.36, The prevailing solution to this issue is to manually evaluate the matched spectra with HQI values near the greatest returned similarity value.31,37, Unfortunately, this proposed solution does not impart any guidance on how many labels, or what lower limit of HQI, should be further evaluated, nor does it give the user any sense of statistical uncertainty in the chosen label. For enhanced workflow clarity and confidence within a label prediction set, we present conformal prediction as a framework to address this need in the microplastic community.

Conformal Prediction

Nearest neighbor leads to smaller mean prediction set sizes than Pearson correlation coefficient. We conducted an analysis using CP with a single distribution of true positive HQI values, utilizing the five labels with more than 10 example spectra in the FLOPP dataset (i.e., PE, PP, PET, PS, and C) as possible spectral classifications. While we display this data herein for simple comparison to the class-conditional results (which were limited by data availability), it should be noted that additional labels can be used with a CP framework and that this addition of labels will result in larger average prediction sets (Figure S3). To illustrate CP in practice, two examples of query FLOPP-e spectra classified using PCC and NN within the conformal prediction workflow and their associated prediction sets are show in Figure 4. We next quantified the mean empirical confidence and prediction set size for both PCC and NN (Figure 5). As expected, the empirical confidence closely aligns with the theoretical value (90%) for both metrics. However, we observed a lower prediction set size using the NN metric compared to PCC. This disparity demonstrates that even metrics yielding the same match can provide different uncertainty quantifications. In other words, prediction sets generated using NN are more efficient than those generated when using PCC. One possible explanation for this difference can be discerned by examining the distributions of the positive matches (i.e., correctly identified) and negative matches (i.e., mismatch of query and reference labels) between spectra of the same FLOPP-e and FLOPP class. With PCC, these distributions significantly overlap, indicating that there are many spectra in the FLOPP-e library with high HQI values relative to incorrect labels (Figure 6). In contrast, with NN, the two distributions are well separated, resulting in fewer spectra with high NN metrics relative to incorrect labels. This concept is closely related to the analysis by Morgado et al., where the authors argue that a slight overlap between the distributions of correlation coefficients from cases of positive and negative matches implies a low false positive rate in the overall method.21 A further explanation for the difference in prediction set sizes is that PCC is an absolute metric whereas NN is a relative metric. To get a high HQI using PCC, the unknown and the reference spectra  need to be closely aligned; however to obtain a high HQI value using NN it is not enough that the two spectra are close, it is also necessary that there is no other reference spectrum that is also close (see Supporting Information section II). Therefore, when using NN, one is less likely to encounter a false positive (mismatched) classification returned in the 90% confidence prediction set than when using PCC.

Figure 4. Example spectra and generated prediction sets using Pearson correlation coefficient and nearest neighbor metrics for FLOPP-e spectra a) PE 11. Green Fragment  and b) PP 8. Orange Fragment. The values in parantheses are the hit quality indeces between query and reference spectra.

Figure 5. Empirical confidence and mean prediction set size results of conformal prediction and class-conditional (CC) conformal prediction using Pearson correlation coefficient and nearest neighbor similarity metrics.

Figure 6. Distribution of HQIs for positive (red) and negative (blue) matches of FLOPP-e spectra matching to FLOPP reference libraries using Pearson correlation coefficient (top) and nearest neighbor (bottom) algorithms. The shaded region on each plot represents the 90% confidence interval.

Class-conditional conformal prediction leads to an increase in mean prediction set size for both similarity metrics. As opposed to the traditional CP methodology, class-conditional CP builds a unique HQI distribution for each included label. CC-CP is particularly useful when the distributions of positive matches between sample and reference spectra differ among the spectral labels. In the case of the five labels used in our analysis, we noted that the HQI distribution of PP is quite distinct from the other labels when treated with Pearson correlation coefficient, as it exhibits true positive scores down to 0.4 in similarity (Figure S4). We hypothesize that the difference in score distributions between classes could be due to the impacts of signal-to-noise ratio, preprocessing steps performed by De Frond et al. in creation of the library, or a greater degree of environmental aging when compared to pristine reference spectra.31,36 As mentioned earlier, CC-CP ensures class-balanced theoretical confidence rather than a distribution average theoretical confidence (Figure S5). This guarantee results in more robust prediction sets at the expense of slightly larger set sizes (Figure 5). Additionally, we compared the performance of PCC and NN within the class-conditional CP framework. Similar to traditional CP, we can observe an advantage of NN over PCC with respect to the mean set size. In addition to empirical coverage and average set size, there are other metrics that help evaluate the performance of CP. For example, the proportion of prediction sets with one or zero classification labels (see Supporting Information).

Comparing the Performance of KnowItAll and the Conformal Prediction Framework

Conformal prediction reduces the mean prediction set size and guarantees confidence when compared to KnowItAll. To showcase the advantage of using conformal prediction in routine environmental microplastic identification, we compared the matching of FLOPP-e polyethylene and polypropylene spectra to all classes of FLOPP spectra with both KnowItAll’s default correlation metric and conformal prediction using PCC and NN metrics. While the analysis pipeline of KnowItAll’s SearchIt function does not quantify uncertainty in spectral identification, we chose to view the results through a conformal-prediction lens. To do so, we equate the proportion of instances that KIA returns the correct label for a query spectrum with the empirical confidence associated with a prediction set generated with CP. Thus, KnowItAll’s “empirical confidence” was defined as the proportion of query spectra per polymer label (FLOPP-e PE and PP) that were matched to a FLOPP spectrum of the correct label with an HQI ≥ 0.7. The observed confidence of KIA (~94% for PE and ~82% for PP) was used to inform the theoretical confidence of the compared conformal prediction methods (94% [α = 0.06] for PE and 82% [α = 0.18] for PP), such that the differences in mean prediction set size were highlighted. As opposed to the mean set size for KIA, here defined as the average number of spectral classes returned with HQI ≥ 0.7 per query spectrum, the use of CP with PCC or NN similarity metrics decreases the number of labels returned and provides a guaranteed uncertainty in the match (Figure 7).

Figure 7. Results of comparison between KnowItAll (KIA) and conformal prediction with PCC and NN similarity metrics in terms of observed confidence and mean set size for a) PE and b) PP.

The mean prediction set size is dependent on the similarity metric, polymer class, and user-defined confidence interval. NN outperforms PCC to give a lower mean prediction set size due to fewer instances of negative matches above the defined quantile, as previously described. Between query spectra classes, the mean set size of predicted labels for PP is lower than for PE. The HQI to reference polymer spectra differ between the FLOPP-e PE and PP spectra, with PE having higher PCC scores to more reference labels than PP (Figure S7 and S8). This observation may explain why PE has a larger mean set size than PP, as labels with higher similarity scores are more likely to be included in the prediction set. Additionally, the results shown in Figure 7 reflect lower confidence associated with PP predictions, meaning that the HQI threshold is less descriptive of the true positive correlation score distribution. The higher HQI score associated with a lower, less descriptive, user-defined confidence level could limit the number of classifications added to the prediction set. Across both polymer classes and confidence levels, CP methods reduced the number of labels returned and guaranteed confidence in the identity classification, streamlining manual interpretation of numerous spectral matches and boosting confidence in identification of an unknown spectrum.

Takeaways for the Microplastic Community

Using the open-access code available on GitHub, a conformal prediction workflow can be used to reduce manual spectral comparison and increase statistical confidence in environmental microplastic labeling. We herein provide a suggested conformal prediction workflow to be used by the microplastic community: First, the user must define a reference library. For CP, there are no assumptions about the reference library, meaning we have confidence guarantees regardless of its composition. However, the quality and efficiency of the prediction sets will depend heavily on the similarity metric, of which the performance is enhanced when have a high-quality reference library. Second, one’s own calibration set is needed. The spectra in the calibration set should ideally be as close as possible to the spectra the user plans to analyze. For example, when analyzing environmental data, collecting and manually labeling an initial dataset that reflects the diversity of the intended analysis would serve as a good calibration set. Although CP produces finite sample guarantees, a larger calibration set yields more stable theoretical confidence and predictions. With a calibration set of around 100 spectra, if our desired confidence level is 90%, we can expect a theoretical confidence between 89% and 91% and an empirical confidence between 85% and 95% (Equation S1 and S2). The difference between the ranges of theoretical and empirical confidence arises from the variability of the actual observations being tested, resulting in a wider range for the empirical confidence. Third, the user can utilize their own reference library and calibration set to make predictions for new environmental samples using the code available on GitHub and the user-guide available as a Supplemental File. The output will be a prediction set for each unknown spectrum at the specified confidence. Finally, the user can use the predictions as follows: prediction sets containing only one label are considered accepted matches, prediction sets with zero labels are considered outliers (indicating that they do not belong to any chemical identity in the reference library), and prediction sets with more than one label undergo expedited manual classification.

The threshold used for accepting a label for an unknown spectrum relies on user-data, similarity metric, and chosen theoretical confidence. As previously noted, the hit quality index between a reference and query spectrum can be similar for multiple reference labels (Figure S7 and S8). Therefore, it is important that a chosen HQI threshold has a statistical guarantee of differentiation between spectral signatures. As shown in Figure 8, when using conformal prediction and Pearson correlation coefficient, the chosen theoretical confidence of the generated results has implications on both the HQI threshold and the mean prediction set size. If one opts for higher theoretical confidence in generated labels, the HQI quantile will be more descriptive of the data and outliers (i.e., lower), and there will be more predicted labels in the set. Therefore, choosing too high of a confidence guarantee could render the prediction sets useless unless subjected to tedious manual evaluation of the matches and lead to false positives, causing an overestimation of MP abundance. On the other hand, choosing too low of a theoretical confidence is accompanied by a higher HQI cut-off and fewer labels in the prediction set that are represented above the high quantile. Here, false negatives could occur because the environmental spectra are too dissimilar from reference spectra, leading to an underestimation of MP contamination. Given this trade-off, researchers must decide on the confidence level they are comfortable with when considering the balance of HQI threshold, prediction set size, and the possibility of over or underestimating MP quantities. Our suggestion would be to choose a confidence value that is both descriptive of most of the calibration set’s HQI distribution (e.g., > 70%) and that returns a mean prediction set size for manageable manual evaluation (e.g., 1–3 labels). Using Figure 8 as a guide, we would choose a theoretical confidence between 70 and 90% based on this suggestion. While the results in Figure 8 are specific to the metrics and data discussed herein, it carries that choosing a single HQI threshold without statistical meaning and applying it to diverse environmental campaigns, as is popular in the wider MP literature, may impact the validity of one’s results.

Figure 8. Hit quality index and mean prediction set size as a function of user-defined theoretical confidence for FLOPP and FLOPP-e data using conformal prediction and Pearson correlation coefficient.

Conformal prediction presents a customizable framework for similarity metric comparison, confidence associated with individual spectra, and guidance on the manual interpretation of spectra with close correlation to two or more reference classes. When comparing similarity metrics, users can employ CP to evaluate the performance of different algorithms for the same dataset. As employed herein, one can assess the efficiency of the metrics through the prediction set sizes they produce with the same confidence level. As discussed earlier, the ability to differentiate between positive and negative matches in one’s labeled calibration data will result in more efficient uncertainty quantification. While workflows to ensure confidence in microplastic matches have been put forth in recent history,18,20,21 they have lacked a measure of statistical uncertainty at the individual spectrum level and do not provide advice on manual evaluation. Rather, the user is only provided with a false negative rate for the entire sample and pass-fail guidance on the single spectrum. With conformal prediction, one obtains confidence in the prediction set returned by a single query spectrum. In the case of more than one predicted class, the analyst has assurance that the correct label for the unknown particle is within the prediction set, and they need only manually evaluate the few labels returned. Therefore, conformal prediction presents a new workflow for the microplastic community to more robustly quantify and  chemically identify environmental microplastics.

Conclusion

Herein, we outlined a flexible framework for statistical uncertainty in environmental MP spectral database searching. Based on our findings from a literature review of  recent microplastic identification data analysis routines and the evaluation of a commercial database matching software, we illustrated the need for guidance on similarity metric comparison, hit quality index thresholding, and confidence in spectral classification. Using both conformal prediction and class-conditional conformal prediction, a reduced mean size of label prediction sets was observed with the nearest neighbor similarity metric as compared to Pearson correlation coefficient. Although class-conditional conformal prediction increased the mean value of labels returned in a prediction set when compared to traditional conformal prediction, class-conditional conformal prediction may decrease the ambiguity of polymer classifications with differing HQI distributions. With a final comparison to a commonly used commercial matching software, we illustrate that conformal prediction streamlines microplastic identification with an associated statistical uncertainty measurement. Finally, we urge the MP community to use our open-access code and user-guide for an adaptable conformal prediction framework to meet their own analytical goals for confidence in similarity metric thresholding and acceptance of an environmental microplastic spectral match.
ASSOCIATED CONTENT

Supporting Information. 
The following files are available free of charge.
Additional details on methodology and results of literature search, similarity metrics, and conformal prediction (PDF)
User-guide for open-access conformal prediction code (PDF)

AUTHOR INFORMATION

Corresponding Author

Anne J. McNeil – Department of Chemistry, University of Michigan, 930 North University Avenue, Ann Arbor, MI 48109-1055, USA; Email: ajmcneil@umich.edu

Ambuj Tewari – Department of Statistics, University of Michigan, 1085 South University Avenue, Ann Arbor, MI 48109-1055, USA; Email: tewaria@umich.edu

Author Contributions

The manuscript was written through contributions of all authors. All authors have given approval to the final version of the manuscript. ‡These authors contributed equally.

Funding Sources

**Any funds used to support the research of the manuscript should be placed here (per journal style).

Notes

The authors declare no competing financial interest.

ACKNOWLEDGMENT

The authors would like to acknowledge the professors and students of the Mapping, Measuring, and Modeling Microplastics in the Atmosphere of Michigan team for their support and thank the College of Literature, Science, and the Arts at the University of Michigan for financial contributions.

ABBREVIATIONS

MP, microplastic; KIA, KnowItAll; CP, conformal prediction; CC-CP, class-conditional conformal prediction; PE, polyethylene; PP, polypropylene; PS, polystyrene; PET, polyethylene terephthalate; PVC, polyvinyl chloride; PEVA, polyethylene vinyl acetate; C, cotton; R, rubber; no ID, unidentified; NN, nearest neighbor; PCC, Pearson’s correlation coefficient; SNV, standard normal variate; HQI, hit quality index; FLOPP, FT-IR library of plastic particles; FLOPP-e,  FT-IR library of plastic particles sourced from the environment.

REFERENCES

Frias, J. P. G. L.; Nash, R. Microplastics: Finding a consensus on the definition. Mar. Pollut. Bull. 2019, 138, 145—147.

Alfaro-Nunez, A.; Astorga, D.; Caceres-Farias, L.; Bastidas, L.; Soto Villegas, C.; Macay, K.; Christensen, J. H. Microplastic pollution in seawater and marine organisms across the Tropical Eastern Pacific and Galápagos. Sci. Rep. 2021, 11, 6424.

Talbot, R.; Chang, H. Microplastics in freshwater: A global review of factors affecting spatial and temporal variations. Environ. Pollut. 2022, 292, 118393.

Cusworth, S. J.; Davies, W. J.; McAinsh, M. R.; Gregory, A. S.; Storkey, J.; Stevens, C. J.  Agricultural fertilisers contribute substantially to microplastic concentrations in UK soils. Commun. Earth Environ. 2024, 5, 7.

Brahney, J.; Hallerud, M.; Heim, E.; Hahnenberger, M.; Sukumaran, S. Plastic rain in protected areas of the United States. Science 2020, 368, 1257—1260.

Cabernard, L.; Roscher, L.; Lorenz, C.; Gerdts, G.; Primpke, S. Comparison of Raman and Fourier Transform Infrared Spectroscopy for the Quantification of Microplastics in the Aquatic Environment. Environ. Sci. Technol. 2018, 52, 13279–13288.

Weisser, J.; Pohl, T.; Heinzinger, M.; Ivleva, N. P.; Hofmann, T.; Glas, K. The identification of microplastics based on vibrational spectroscopy data – A critical review of data analysis routines. TrAC, Trends Anal. Chem. 2022, 148, 116535.

OPUS Package: SEARCH & IDENT. https://www.bruker.com/en/products-and-solutions/infrared-and-raman/opus-spectroscopy-software/search-identify.html (accessed 2024-02-20).

FTIR Analysis Software. https://www.thermofisher.com/us/en/home/industrial/spectroscopy-elemental-isotope-analysis/molecular-spectroscopy/fourier-transform-infrared-spectroscopy/software.html (accessed 2024-02-20).

KnowItAll Analytical Edition Software. https://sciencesolutions.wiley.com/knowitall-analytical-edition-software/ (accessed 2024-02-20).

Thompson, R. C.; Olsen, Y.; Mitchell, R. P.; Davis, A.; Rowland, S. J.; John, A. W. G.; McGonigle, D.; Russel, A. E. Lost at Sea: Where Is All the Plastic? Science 2024, 304, 838.

Abbasi, A.; Sadeghi, P.; Abadi, Z. T. R. Characterization of microplastics in digestive tract of commercial fish species from the Oman Sea. Mar. Pollut. Bull. 2023, 197, 115769.

Clark, L.; Allen, R.’ Botterell, Z. L. R.; Callejo, B.; Godley, B. J.; Henry, C.; Santillo, D.; Nelms, S. E. Using citizen science to understand floating plastic debris distribution and abundance: A case study from the North Cornish coast (United Kingdom). Mar. Pollut. Bull. 2023, 194, 115314.

Miserli, K.; Lykos, C.; Kalampounias, A. G.; Konstantinou, I. Screening of Microplastics in Aquaculture Systems (Fish, Mussel, and Water Samples) by FTIR, Scanning Electron Microscopy–Energy Dispersive Spectroscopy and Micro-Raman Spectroscopies. Appl. Sci. 2023, 13, 9705.

Renner, G.; Schmidt, T. C.; Schram, J. A New Chemometric Approach for Automatic Identification of Microplastics from Environmental Compartments Based on FT-IR Spectroscopy. Anal. Chem. 2017, 89, 12045—12053.

Lopez-Rosales, A.; Ferreiro, B.; Andrade, J.; Ferndandez-Amado, M.; Gonzalez-Pleiter, M.; Lopez-Mahia, P.; Rosal, R.; Muniategui-Lorenzo, S. A reliable method to determine airborne microplastics using quantum cascade laser infrared spectrometry. Sci. Total Environ. 2024, 913, 169678.

Jung, M. R.; Horgen, D. F.; Orski, S. V.; Rodriguez, V. C.; Beers, K. L.; Balazs, G. H.; Jones, T. T.; Work, T. M.; Brignac, K. C.; Royer, S. J.; Hyrenback, D. K.; Jensen, B. A.; Lynch, J. M. Validation of ATR FT-IR to identify polymers of plastic marine debris, including those ingested by marine organisms. Mar. Pollut. Bull. 2018, 127, 704—716.

Primpke, S.; Lorenz, C.; Rascher-Friesenhausen, R.; Gerdts, G. An automated approach for microplastics analysis using focal plane array (FPA) FTIR microscopy and image analysis. Anal. Methods 2017, 9, 1499—1511.

Primpke, S.; Wirth, M.; Lorenz, C.; Gerdts, G. Reference database design for the automated analysis of microplastic samples based on Fourier transform infrared (FTIR) spectroscopy. Anal. Bioanal. Chem. 2018, 410, 5131—5141.

Choy, C. A.; Robinson, B. H.; Gagne, T. O.; Erwin, B.; Firl, E.; Halden, R. U.; Hamilton, J. A.; Katija, K.; Lisin, S. E.; Rolsky, C.; Van Houtan, K. S. The vertical distribution and biological transport of marine microplastics across the epipelagic and mesopelagic water column. Sci. Rep. 2019, 9, 7483.

Morgado, V.; Palma, C.; Bettencourt da Silva, R. J. N. Microplastics identification by infrared spectroscopy – Evaluation of identification criteria and uncertainty by the Bootstrap method. Talanta 2021, 224, 121814.

Akdogan, Z.; Guven, B. Microplastics in the environment: A critical review of current understanding and identification of future research needs. Environ. Pollut. 2019, 254, 113011.

De Frond, H.; Rubinovitz, R.; Rochman, C. M. μATR-FTIR Spectral Libraries of Plastic Particles (FLOPP and FLOPP-e) for the Analysis of Microplastics. Anal. Chem. 2021, 93, 15878—15885.

Wiley KnowItAll Optimized Corrections. https://help.knowitall.com/index.htm#t=mergedProject s%2FID_Expert%2FOptimized_Corrections.htm (accessed 2024-02-20).

Stein, S. E.; Scott, D. R. Optimization and Testing of Mass Spectral Library Search Algorithms for Compound Identification. J. Am. Soc. Mass Spectrom. 1994, 5, 859– 866.

R. Xu 2008 Xu, R.; Wunsch, D.C. Proximity Measures. In Clustering; 2008; pp 15-30.

Renner, G.; Nellessen, A.; Schwiers, A.; Wenzel, M.; Schmidt, T. C.; Schram, J. Data preprocessing & evaluation used in the microplastics identification process: A critical review & practical guide. TrAC, Trends Anal. Chem. 2019, 111, 229—238.

Barnes, R. J.; Dhanoa, M. S.; Lister, S. J. Appl. Spectrosc.1989, 43, 772−777.

Cowger, W.; Steinmetz, Z.; Gray, A.; Munno, K.; Lynch, J.; Hapich, H.; Primpke, S.; De Frond, H.; Rochman, C.; Herodotou, O. Microplastic Spectral Classification Needs an Open Source Community: Open Specy to the Rescue! Anal. Chem. 2021, 93, 7543—7548.

Primpke, S.; Cross, R. K.; Mintenig, S. M.; Simon, M.; Vianello, A.; Gerdts, G.; Vollertsen, J. Toward the Systematic Identification of Microplastics in the Environment: Evaluation of a New Independent Software Tool (siMPle) for Spectroscopic Analysis. Appl. Spectrosc. 2020, 74, 1127—1138.

Schmidt, L. K.; Bochow, M.; Imhof, H. K.; Oswald, S. E. Multi-temporal surveys for microplastic particles enabled by a novel and fast application of SWIR imaging spectroscopy – Study of an urban watercourse traversing the city of Berlin, Germany. Environ. Pollut. 2018, 239, 579—589.

Schymanski, D.; Oßmann, B. E.; Benismail, N.; Boukerma, K.; Dallmann, G.; von der Esch, E.; Fischer, D.; Fischer, F.; Gilliland, D.; Glas, K.; Hofmann, T.; Kappler, A.; Lacorte, S.; Marco, J.; Rakwe, M. E. L.; Weisser, J.; Witzig, C.; Zumbulte, N.; Ivleva, N. P. Analysis of microplastics in drinking water and other clean water samples with micro-Raman and micro-infrared spectroscopy: minimum requirements and best practice guidelines. Anal. Bioanal. Chem. 2021, 413, 5969—5994.

Boruta, M. FT-IR Search Algorithm – Assessing the Quality of a Match. Spectroscopy 2012, 27, s26—s33.

Acik, G.; Cansoy, C. E.; Kamaci, M. Effect of flow rate on wetting and optical properties of electrospun poly(vinyl acetate) micro-fibers. Colloid Polym. Sci. 2018, 297, 77—83.

Rolere, S.; Liengprayoon, S.; Vaysse, L.; Sainte-Beuve, J.; Bonfils, F. Investigating natural rubber composition with Fourier Transform Infrared (FT-IR) spectroscopy: A rapid and non-destructive method to determine both protein and lipid contents simultaneously. Polym. Test. 2015, 43, 83—93.

Gonzalez, V.; Guerrero, C.; Oritz, U. Chemical structure and compatibility of polyamide-chitin and chitosan blends. J. Appl. Polym. Sci. 2000, 78, 850—857.

Brandt, J.; Bittrich, L.; Fischer, F.; Kanaki, E.; Tagg, A.; Lenz, R.; Labrenz, M.; Brandes, E.; Fischer, D.; Eichhorn, K.-J. High-Throughput Analyses of Microplastic Samples Using Fourier Transform Infrared and Raman Spectrometry. Appl. Spectrosc. 2020, 74, 1185—1197.

Vovk, V. Conditional Validity of Inductive Conformal Predictors. J. Mach. Learn. Res. 2012, 25, 475-490.

TOC GRAPHIC